Complete (

# Slot-Stitching

SPV.0060.

905-_____-_____

Steel Tie Bar

- Diary entry required.  Bid Item ID: _______________

  - Accept in accordance with CMM 8-50 Exhibit 1, Concrete Reinforcement, Tie Bars

  - Certified report of test or analysis required for all heat numbers

  - Document all heat numbers

Patch Material

- Diary entry required.  Bid Item ID: _______________

  - Verify product and manufacturer are on approved list:

    - Portland Cement Concrete » Rapid set concrete repair materials

Caulking Filler

- Diary entry required.  Bid Item ID: _______________

  - Verify compatibility with patch material

Chairs

- Diary entry required.  Bid Item ID: _______________

  - Sample chair required prior to use

Cure

- Diary entry required.  Bid Item ID: _______________

  - Verify product and manufacturer are on approved list:

    - Portland Cement Concrete » Concrete curing compounds » PAMS-Based Curing Compounds

| Item No. | Description | Plan Quantity | Final Quantity |
| --- | --- | --- | --- |
| SPV.0060. | Slot-Stitching | EACH | EACH |