Complete (

# Storm Sewer Pipe Reinforced Concrete

# Class V (Inch) Jacked

SPV.0090.

905-_____-_____

#### Buy America

Certification documents for steel reinforcement items must denote compliance to all elements of Buy America provisions.

Pipe

- Diary entry required. Bid Item ID: _______________

  - Record pipe markings in basis for acceptance: manufacturer and plant location, date of manufacture, and specification designation.

  - Record which pipe sections are tied.

- Verify that the manufacturer & plant are on the approved list.

- Each shipment will have a loading document. Retain with material archive.

- Buy America compliance from manufacturer is required.

Mortar Joint Connection

Mortar Cement – Type S

- Diary entry required. Bid Item ID: _______________

  - Manufacturer’s certification of compliance is required.

  - Record percentage of components.

Portland Cement

- Diary entry required. Bid Item ID: _______________

  - Manufacturer’s certification of compliance is required.

  - Record percentage of components.

Masonry Cement – Type S

- Diary entry required. Bid Item ID: _______________

  - Manufacturer’s certification of compliance is required.

  - Record percentage of components.

Hydrated Lime

- Diary entry required. Bid Item ID: _______________

  - Manufacturer’s certification of compliance is required.

  - Record percentage of components.

Bagged Utility Mortar

- Diary entry required. Bid Item ID: _______________

  - Verify product is on the approved products list.

  - Ensure bags have label matching approved products list.

Mortar Sand

- Diary entry required. Bid Item ID: _______________

  - Sample in accordance with CMM 8-50 Exhibit 1, Mortar, Mortar Sand

Water

- Diary entry required. Bid Item ID: _______________

  - Record clarity of water.

## Backfill

## Foundation Backfill

- Diary entry required.  Bid Item ID: _______________

  - Record material type.

  - Sample in accordance with CMM 8-50 Exhibit 1, Aggregates – Project Testing, Storm Sewer Backfill Foundation

- Contractor to supply sample gradation, plasticity index, and liquid limit results to engineer prior to placing material. Engineer may waive contractor testing for known sources.

Trench Backfill

- Diary entry required.  Bid Item ID: _______________

  - Record material type.

  - Sample in accordance with CMM 8-50 Exhibit 1, Aggregates – Project Testing, Storm Sewer Backfill Foundation

| Item No. | Description | Plan Quantity | Final Quantity |
| --- | --- | --- | --- |
| SPV.0090. | Storm Sewer Pipe Reinforced Concrete Class V (Inch) Jacked | LF | LF |